## Slide 1
Results and Discussion
Introduction and motivation
Device Simulation
Conclusions
References
Terahertz GaN Schottky varactor based on inverted trapezoidal metal-brim terminal structure
Abstract
GaN Schottky barrier varactor based on inverted trapezoidal metal-brim terminal structure was first proposed for terahertz frequency multiplier application. Compared with conventional varactor, simulation results show that inverted trapezoidal metal-brim structure effectively increases capacitance modulation capability, reduces the tunneling current and improve the breakdown characteristics. Thus, the proposed terminal structure could optimize the performance of GaN terahertz frequency multiplier, which could be widely used in Terahertz communication regions, imaging systems, radiometers, and so on.
High output power and high efficiency solid state terahertz sources were seriously required in THz regions
GaN material show many advantages in Terahertz application
THz GaN-based Schottky barrier varactor showing new characteristics
Metal-brim terminal structure has the advantages of reducing leakage current and eliminating edge capacitance effect
Luwei Qi, Weibo Wang, Hongqi Tao, Xuming Yu, Jin Meng, Dehai Zhang
Nanjing Electronic Devices Institute
GaN bulk-material structure:
- a 0.3μm-thick lightly doped n-type GaN layer
- a 3μm-thick heavily doped n-type GaN layer
- a 2μm-thick high resistance GaN layer
- SiC substrate
Sentaurus TCAD simulation:
DC characteristics:
The simulated I-V curve of GaN varactors with three shapes of metal-brim structure display the similar DC characteristics.
C-V simulation results and Current density distribution:
Nonlinear C-V characteristics:
The inverted trapezoidal structure could increase the capacitance modulation ratio, thus improving the conversion efficiency of nonlinear capacitance in frequency multiplier applications.
This was because the inverted trapezoidal structure increases the rate of depletion layer charges with voltage bias.
[1] Marso M. GaN for THz sources[C]//The Eighth International Conference on Advanced Semiconductor Devices and Microsystems. IEEE, 2010, 147-154.
[2]Chattopadhyay G. Technology, capabilities, and performance of low power terahertz sources [J]. IEEE Transactions on Terahertz Science and Technology, 2011, 1(1): 33-53.
[3]Mittleman D M. Twenty years of terahertz imaging[J]. Optics express, 2018, 26(8): 9417-9431.
[4]Dhillon S S, Vitiello M S and Linfield E H. The 2017 terahertz science and technology roadmap[J]. Journal of Physics D: Applied Physics, 2017, 50(4): 043001.
[5]Siles J V, Grajal J. Capabilities of GaN Schottky multipliers for LO power generation at millimeter-wave bands[C]. 19th International Symposium on Space Terahertz Technology. 2008:504-507.
[6]Liang S, Song X and Zhang L. A 177–183 GHz High-Power GaN-Based Frequency Doubler With Over 200 mW Output Power[J]. IEEE Electron Device Letters, 2020, 41(5): 669-672.
[7]Tian C, Yang H, Dong J, Huang J and Zhang H. Desigh and Fabrication of GaAs Planar Schottky Varactor Diode with the Exponential Doping Structure [J]. Chinese Journal of Electron Devices, 2011, 34(1): 29-32.
[8]Qi L, Meng J and Liu X. Optimization of terahertz monolithic integrated frequency multiplier based on trap-assisted physics model of THz Schottky barrier varactor[J]. Chinese Physics B, 2020, 29(10): 104212.
Field plate structure could increase the breakdown voltage, but it could not completely eliminate the leakage current at the junction edge.
The metal-brim structure showed the best breakdown voltage by eliminating the edge leakage effect.
The inverted trapezoidal metal-brim terminal structure provided better nonlinear C-V characteristics and breakdown characteristics.
This terminal structure provides a feasible scheme for the optimization of THz GaN-based multipliers.
Begin
Device structure
Define material
Doping and meshing
Boundary conditions
Device Modeling
Solving the equilibrium states
Solving Drift-diffusion equations
Quasi-static scanning
convergence
yes
End
no
Results
Inverted trapezoid
Rectangle
Trapezoid